**Oak Protect Technical information**

TECHNICAL DETAILS

 Appearance: cloudy white liquid

Odor: faint wax odour

Density: 1

Viscosity: 25”/DIN 4mm.

PH: 8.4

Shelf life: 2 years in a closed container

PREPARATION

The surface must be new or cleaned and sanded (grit 120); If you are working on old wood please carefully remove or sand the old layers first.

INSTRUCTIONS FOR USE

 Stir very well before and during use.

Apply undiluted with a brush or roller

For untreated surfaces treat at least twice. If the surface continues to absorb, it is advisable to continue the treatment until the surface is saturated leaving a milky residue.

The number of coats may slightly affect the gloss.

All materials used for application can be cleaned with water.

DRYING TIME

Dust dry after 4 hours, second coat after 24 hours.

PRACTICAL COVERAGE

 10 m2/litre depending on the requirements of the surface.

MAINTENANCE CYCLE

Please apply to untreated wood twice. After approx. 3 years: when the surface decreases water repellence reapply.

PACKAGE AND STORAGE

2.5L tin

Shelf life: 2 years in closed packaging Dry and frost-free storage

SAFETY

The impregnating wax is completely natural, free of solvents and therefore does not require any special treatment safety regulations. We always recommend that you take note of the safety data sheet. Keep out of reach of children.